A new Photon Calorimeter with high energy and time resolutions was needed for the KOPIO experiment that was planned to be carried out at the BNL (USA). Because of that the scientists of Yale University Elementary Particle Interaction group (YALE-EPI) and IHEP (Protvino) have designed a fine sampling module of this calorimeter satisfying the above requests. As the base the «Shashlyk» type module design was taken which is relatively cheap (in comparison with calorimeters based on mono-crystals) and simple for manufacturing. The whole work consisted of the following stages:

- The module design

The sensitive volume of the module consists of 300 layers. Each layer has a scintillation tile with thickness of 1,5 mm and a lead plate with the thickness of 275 micrometers. The module construction is shown in Fig.1. Module parameters are presented in Table 1. The photo of the last version of the module is shown in Fig.2.

Fig.1

| Lateral segmentation | 110´110 mm2 |
| --- | --- |
| Scintillator thickness | 1.5 mm |
| Gap between scintillator tiles | 0.300 mm |
| Lead absorber thickness | 0.275 mm |
| Number of the absorber layers (Lead / Scint.) | 300 |
| WLS fibers per module | 72 ´ 1.6 m = 115 m |
| Fiber spacing | 9.3 mm |
| Holes diameter in Scintillator / Lead | 1.3 mm / 1.4 mm |
| Diameter of WLS fiber (Y11-200MS) | 1.0 mm |
| Fiber bundle diameter | 14.0 mm |
| External wrapping (Tyvek paper) | 150 m |
| Effective Xo | 34.0 mm |
| Effective RM | 59.8 mm |
| Effective density | 2.75 g/cm3 |
| Active depth | 540 mm (15.9 Xo) |
| Total depth (without photo detector) | 650 mm |
| Total weight | 18.0 kg |

Table 1.

Parameters of the Photon Calorimeter module for the KOPIO experiment.

Fig. 2

Each scintillation tile and lead plate have the sizes of 109,7109,7 mm2 (Fig. 3). Each scintillation tile and lead plates have 144 holes (diameter of 1,3 mm) with a step of 9,3 mm. 144 wavelength shifting (WLS) fibers (KURARAY, Y11-200MS, 1 mm diameter) are inserted through the holes.

Fig. 3

Scintillation tile.

Each scintillation tile has a four special pins and deepening (corresponding each other) for mutual fixation (similar to LEGO). These pins are also used for providing the required gap between lead and scintillation tiles which prevent the formation of an optical contact between them (that usually leads to a loss of light).   The scintillation light from the tiles is reemitted into a wavelength region of about 480 nm by the WLS-fibers. The module is wrapped with a reflective Tyvek paper. On the opposite side (from a photodetector) of the module WLS-fibers forms loops. These constructive elements increase the light output and homogeneity in Calorimeter. Thus, the whole reemitted and trapped light is transmitted to photodetector via the WLS-fibers. The WLS-fiber ends are coupled to an avalanche photodiode (APD) having the quantum efficiency of 93% in the green wavelength region.

The module assemblage setup is shown in Fig. 4.

Fig. 4

Fig. 5

After assemblage each module undergoes a cycle of loading (there is a need of 3-4 cycles of loading with a force up to 800 kg) for preventing any future shrinkage. Such procedure stabilizes the length of the module sensitive volume with accuracy of about +/- 1mm. The whole module is then fixed by 4 steel roads with 1,2 mm diameter (under loading).

After that the ends of WLS-fibers was put in a bundle, was cut and then polished. The module at this stage of assemblage is shown in Fig. 5. The module ends have light-tightened covers. The lateral module sides are wrapped with a black paper (see Fig. 2).

- Choice of scintillator

Material for scintillators should be cheap and available in large volume on the market because is needed about 9 tons of scintillator tiles for the KOPIO experiment. That is why the polystyrene (PS) was chosen as the basis for the scintillator.  Samples of available (on the market) PS were investigated with the aim of choosing the best transparent trade mark in the wavelength region 300-420 nm because in this region the scintillation light is emitted, reemitted and is transferred to WLS-fibers. Some results of these investigations are shown in Fig. 6.

Fig. 6

Granulated PS ВАSF-143E и ВАSF-165H trade marks were chosen as the basis for scintillation tiles. Special technology was worked out for the process of introduction of scintillation and wavelength shifting dopants into our scintillator. So, granulated PS, scintillation and wavelength shifting dopants (fluors) were drying at the temperature of 700 С during 1 hour. After that they were mixed in a special barrel during 1,5 hour.

The mixture of them were put into a plastic injection molding machine DEMAG for molding under a high pressure.  The regimes of injection-molding processes were chosen in such a way that the deviation of geometrical parameters of our scintillator tiles was within the required limits. Chemical formula and optimal concentrations of scintillator dopants were optimized with respect to the scintillator light yield, the light attenuation etc.

Some results of these measurements are presented in Table 2.

| Scintillator: PS+Fluor1+Fluor2, Manufacturer | Light yield (% of Anthracene) | Attenuation Length (cm) | Light yield of MIP, ph.el. per tile | Simulated light collection efficiency |
| --- | --- | --- | --- | --- |
| PSM115 +1.5% pTP +0.04% POPOP, TECHNOPLAST | 53 ± 6 | 4.0 ± 0.3 | 4.4 ± 0.3, 100% | 0.134 ± 0.013, 100% |
| BASF-158K +1.5% pTP +0.04% POPOP, IHEP | 56 ± 6 | 4.9 ± 0.4 | 5.6 ± 0.3, (127 ± 10)% | 0.170 ± 0.017, (127 ± 13)% |
| BASF-165H +1.5% pTP +0.04% POPOP, IHEP | 56 ± 6 | 6.1 ± 0.5 | 6.4 ± 0.3 (145 ± 10)% | 0.191 ± 0.019, (143 ± 14)% |
| BASF-143E +1.5% pTP +0.04% POPOP, IHEP | 54 ± 6 | 6.8 ± 0.5 | 7.1 ± 0.3, (161 ± 10)% | 0.215 ± 0.021, (160 ± 16)% |

Table. 2

Granulated PS BASF-143E with pTP as the scintillation and POPOP as the wavelength shifting dopants turned out to be the best for the mass production of plastic scintillator tiles. These components provide a high level of light yield (up to 60% of that of the anthracene) with decay times of about 2,3 ns. What is more that а wavelength shifting dopant РОРОР having its maximum light emission at 420 nm well coincides with the absorption spectrum of Y-11 WLS-fibers. These dopants are relatively cheap, can be produced in large volumes, and can provide up to 7% better light yield then other dopants.

00000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000000003. Choice of injection-molding equipment.

The technology of high quality scintillator plates production was worked out in IHEP (Protvino) with the use of DEMAG plastic injection molding machines. Some characteristics of the DEMAG machines, that were bought for mass production of scintillator tiles for the KOPIO experiment, are presented in Table 3.

| Plastic Injection Molding Machine model | EТ 80/420 – 310 DEMAG, Germany | EТ 200/560 – 1450 DEMAG, Germany |
| --- | --- | --- |
| Clamping force, ton. | 80 | 200 |
| Screw diameter, mm | 35 | 60 |
| Injection pressure, kg/cm2 | 2020 | 1905 |
| Injection capacity, cm3 | 168 | 763 |
| Platen dimension, mm | 600 х 600 | 830 х 830 |
| Distance between tie-bars, mm | 420 х 420 | 560 х 560 |

Table 3

The DEMAG machine EТ 80/420 – 310 is shown in Fig. 7. Fig.8 show the mold installed inside the plastic injection molding machine. The DEMAG plastic injection molding machines allow to control the parameters of scintillator tiles during the injection-molding process with high accuracy (about 1% for light output of scintillation tiles, for example).

Fig. 7

Fig.8

The mold for scintillator tile production (shown in Fig.9) was designed and manufactured in IHEP. High quality of the mold polished surfaces provides the improvement of the light output from the scintillation tiles. The mold has resource at about 500 000 cycles.

Lead plates were manufactured at IHEP. Thin lead sheets were calibrated on special equipment. Then these sheets were cut into semimanufactures. Formation of lead plates (with holes) from semimanufactures were performed with the use of a stamp presented in Fig.10.

There also was designed and manufactured some additional molds that needed for production of some constrictive elements of the Calorimeter (compression plates, forward and back light protective covers).

Fig. 9

Fig. 10

4. Quality control

The quality control of our scintillator tiles were carried out in two ways.  The first way was a fast «on-line control» that was carried out immediately after the tile production on injection molding machine. A one tile from a batch of 50 was checked. The tile was excited by 90Sr radioactive source. A setup for the quality control of scintillation tiles is shown in Fig.11.

The photocurrent was measured (during 20 s). Then the measured photocurrent was compared with that of a reference tile.

In a second way of the quality control a batch of about 20 tiles were excited by minimum ionizing particles (MIP). The amplitude spectrum from the batch was measured and the number of photoelectrons was determined. Then the measured number of photoelectrons was compared with that of a reference plate that they show the quality of plate surfaces (Fig. 12). In both cases the data acquisition (DAQ) software based on Labview  ver. 4.x for Windows acquires and organizes data from the CAMAC using the crate controller K331 and PC interface card were used.

Fig. 11

The quality control setup using 90Sr

radioactive source.

Fig. 12

The quality control setup using MIP. A typical amplitude spectrum is shown for a batch of 21 scintillation tiles under the MIP excitation.

Fig. 13 presents the reflection efficiencies of some reflectors as a function of the wavelength. Fig. 14 presents the reflection efficiencies of some types of the Tyvek papers. The Tyvek 1055B was chosen as the external reflector for calorimeter module.

Fig.13

Fig. 14

Fig. 15 shows the results of homogeneity of light output measurements from a scintillator tile (with 90Sr radioactive source) having different reflectors.

Fig. 15

The results of the homogeneity light output measurements from a scintillation tile

5.  Module testing

After the end of assemblage procedure all modules, installed vertically, were tested under MIP excitation. The results of these measurements were recorded in a special data acquisition base.

Data acquisition (DAQ) software based on Labview  ver. 4.x for Windows acquires and organizes data from the CAMAC using the crate controller K331 and PC interface card. Dynamic link library “conndb.dll” (see Fig.16) was designed for data transfer into database occurs through open data base connectivity (ODBC).

MySQL was chosen as database system because of it’s availability, licensing and the combination of Linux, Apache, PHP, ROOT, mySQL is hard to beat.

Database “kopio” has the table “modules” (see Table 4) where stores necessary information measurements: uid – unique number, name – module name, date – date and time at the end of the measurement, descrip – description, for example, cosmic, led …, hist – data storage from ADC, histparam – results of the processing from field “hist”, startdata – starting condition for processing result.

User can obtain access to database “kopio” by means of graphical interface (see Fig. 18) or web interface (see Fig. 19).  Graphical user and web interface make the construction of complex queries easy even for user with no database experience. Another capability of this interface is the processing and visualization of selected data.

User works with web interface through web browser (see Fig. 17).  User sends request for server.  Web server Apache takes request. Apache analyses request and call PHP or Carrot (ROOT Apache module. See http://carrot.cern.ch/) for processing of this request. Finally, the Apache to give web page from result  realized software code.

Table 4. Structure database “kopio” – table “modules”

| Name | Type | NULL | Default | Extra |
| --- | --- | --- | --- | --- |
| Uid | int(6) unsigned |  |  | Primary key, unique, Auto_increment |
| Name | Varchar(255) |  |  |  |
| Date | Datetime |  | 0000-00-00 00:00:00 |  |
| Descrip | Varchar(255) | YES |  |  |
| Hist | Blob |  |  |  |
| Histparam | Varchar(255) | YES |  |  |
| Startdata | Varchar(255) | YES |  |  |

Fig. 16

Block scheme of DAQ for the KOPIO modules

Fig. 17

Structured scheme of the client/server system in context web interface

Fig. 18

Graphical user interface for database “kopio”

Fig. 19

Example data processing by means of web interface

6. Calorimeter prototype testing

The 9 (3x3) modules was  assembled as Calorimeter prototype. Two prototypes of Calorimeter having different reflective coatings are shown in Fig. 20.

Fig. 20

The prototypes of Photon Calorimeter.

A prototype of Photon Calorimeter was tested in a photon beam of the BNL (USA). The experimental setup for prototype measurement is shown in Fig.21. An amplitude spectrum from the prototype measured under 250 MeV photon beam is shown in Fig. 22. The energy resolution of ~3%/E (GeV) and high light output were achieved for this prototype having the fine sampling structure and an APD with the quantum efficiency of 93%. The results are presented in Fig.23. The time resolution of the prototype is shown in Fig.24.

Fig. 21

Fig. 22

Fig. 23

Fig. 24

- G.S. Atoyan, et. al., Nucl. Instr. and Meth., A 320 (1992) 144

- A.A. Durum, et. al., IHEP, Preprint 99-6 (1999), Protvino

- S.P. Stoll, BNL, PHENIX Note #245 (1996)

- G.S. Atoyan, et. al., ES, “Development of Shashlyk Calorimeter for KOPIO” (2003) ?